## Slide 1
1.1 Problem Description: Derisking CO2​ Catalytic Deoxygenation
While catalytic deoxygenation is a mature technology in industries like urea and chlor-alkali production, it has not yet been deployed at industrial scale for post-combustion CO2​ capture streams. The primary technical challenge lies in ensuring the long-term stability of noble metal catalysts (Platinum or Palladium) when exposed to the unique conditions of captured CO2​, specifically high water content (up to 40 mol%) and trace contaminants like amines, SOx​, and aldehydes
A critical risk being addressed through experimental study is hydrothermal ageing. High water partial pressure and relative humidity can cause the catalyst's alumina support to reorganize into boehmite, potentially leading to the physical disintegration of the catalyst bed and loss of performance
1.2 Project Background
As part of its strategy to reach net-zero emissions by 2050, Shell is implementing large-scale Carbon Capture and Storage (CCS) projects. When CO2​ is captured from combustion flue gases using amine-based technologies (like CANSOLV), the resulting stream contains trace levels of oxygen (O2​). This O2​ must be removed to meet stringent pipeline specifications (typically <10 ppmv) to prevent corrosion and maintain infrastructure integrity. The first industrial application for this technology is the Moerdijk CCS project, which targets the capture of 800 ktonnes of CO2​ per annum
1.3 Business Need and Opportunity
The successful derisking of this purification step is vital to:
Enable CO2​ Transport and Storage: Meeting pipeline specs is a non-negotiable requirement for the Moerdijk CCS project and future developments like Quest, Acorn, and Charters.
Cost Optimization: Establishing a "derisked operating window" allows for the selection of off-the-shelf catalysts from multiple vendors (Clariant, BASF, Johnson Matthey), ensuring competitive pricing and interchangeability.
Future-Proofing: While current targets are <10 ppmv O2​, the technology has the potential to reach <1 ppmv for future, more stringent project requirements

## Slide 2
2.The Need for a Collaborative Approach
The complexity of this challenge necessitates a partnership between the Gas Processing department and the Catalyst Technology team because it requires a multi-disciplinary solution:
Process Design vs. Experimental Validation: The Gas Processing team manages the overall system integration, compression stages, and vendor engagement. However, because vendors lack experience with these specific high-moisture and contaminant-rich environments, internal experimental tests (long-term stability and hydrothermal studies) are required to validate and expand the operating envelope.
Specialised SME Input: Addressing risks like catalyst poisoning by SOx​ or amines and potential side reactions (like methanation or NOx​ hydrogenation) requires deep expertise from Catalyst Technology Subject Matter Experts (SMEs) to develop the necessary technical specification sheets and mitigation strategies
2.1 Collaboration Framework

## Slide 3
3. Joint Approach & Methodology
Show how both teams worked together.
Phases
Problem Identification
Requirement Alignment
Joint Development
Testing & Validation
Business Deployment
Visual: Timeline or workflow arrow.
Highlight:
Regular review meetings
Knowledge sharing sessions
Joint decision-making
Feedback loops